## Slide 1: Field Dynamics in Superconducting (Accelerator) Magnets
Luca.Bottura@cern.ch
CAS on Superconductivity, Erice, May 8-17, 2002
Theory and Reality…

## Slide 2: Theory…
It’s 2016…
… nuclear war lurks between India and Pakistan …
… Jill, a wonderful blonde, dicovers a new ceramic SC well above RT (Cu-Pt-Sc mix, the one that does not explode) …
… large Pt and Sc reserves found in Sri-Lanka…
… Jill wins the Nobel Prize in Chemistry and Physics …
… sees instant widespread applications of SC (B$ over B$)
… and saves the world from nuk’ing …
T. Clancy, Carrier: a guided tour of an aircraft carrier, Berkeley Publications, 1999

## Slide 3: … and Reality
It’s 2002…
… nuclear war lurks between India and Pakistan …
… the workhorse of superconducting technology is (still) NbTi, discovered between ‘55 and ‘65…
… never awarded a Nobel Prize in Chemistry nor Physics …
… the largest-scale application of superconductivity will be the LHC, costing a mere 2 B$ and scheduled to come into operation for 2007 (theory or reality ?) …
… will it save the world from nuk’ing ? Maybe !

## Slide 4: Plan of the lecture:
Look at accelerator magnets and demonstrate by examples (reality):
  Coupling current effects
  Current distribution
  Field decay and snap-back in accelerator magnets
These effects are important when looking at
  high precision (better than 0.1 %)
  extreme operating conditions (high ramp-rate)
  because they affect reproducibility
A virtual reality demo

## Slide 5: Cable coupling currents
SC Rutherford cable in transverse field
 dB/dt
cross-over contact Rc
eddy current loop
Ieddy
x
w
t
=w/t

## Slide 6: Cable coupling currents
Eddy current Ieddy (A):
Magnetic moment per unit volume Meddy (T):
Heat loss Peddy (W/m):
Ieddy  0.8 A
Meddy  3 mT
Peddy  0.5 mW/m
LHC cable (w=15 mm, t=2 mm, =7.5) with Rc=15and dB/dt = 7 mT/s:

## Slide 7: Coupling currents in a magnet
eddy currents in a LHC dipole (inner layer)
  dI/dt = 10 A/s (dB/dt  7 mT/s), Rc = 15 
dB/dt parallel to cable
dB/dt normal to cable
Ieddy 0.6 A
Ieddy 0.05 A

## Slide 8: Field advance
Meddy generates a field that adds to the background field (advance) proportional to:
  dB/dt
  1/Rc
linear ramps
time
I
I
B
2B(dB/dt,1/Rc)
order of few 10-4

## Slide 9: Field and harmonics
not bad
from AC loss measurement
loss and field measurements in LHC models
mmmh…
what is this ???

## Slide 10: Rc distribution
eddy current in a LHC dipole with Rc variations
  dI/dt = 10 A/s (dB/dt  7 mT/s)
  Rcleft = 17.5 
  Rcright = 12.5 
Ieddy 0.6 A
Ieddy 0.8 A
right-left asymmetric

## Slide 11: Non-allowed harmonics
non-allowed harmonics are produced, their magnitude depends on the Rc distribution
Rc  5 

## Slide 12: Reverse engineering…
SSC dipole prototype DCA312
A. Devred, T. Ogitsu, Ramp rate sensitivity of SSC Dipole Magnet Prototypes, Frontiers of Accelerator Magnet Technology, World Scientific, 184, 1996
variation in z can also be significant
as much as a factor 5 variation !

## Slide 13: Why is it important ?
field distortion is a headache for HEP
  LHC dipoles during 10 A/s ramps and Rc = 15 
    b1 = 5.4 x 10-4  Q = 0.054 vs. 0.003 allowed
    b3 = 1.0 x 10-4   = 52 vs. 1 allowed
solution
  tolerate and correct (measure, measure, measure …)
  slow-down (remember dB/dt dependence) …
  Rc control, e.g. LHC Rc > 15 , aiming at 20 
    Ag-Sn, Sn-Pb, Cu-Ni, Ni, Cr-coatings (few m, bath or electrodeposition)
    Cu-oxide formation (ageing of cable in a humid warehouse)
    dirt, Mobil-1, soap
    core for a Rutherford cable
    any brighter ideas ? Must be compatible with manufacturing process !
Notes: Both uncorrected snap-back and ramp could be extremely critical for beam performance. The comparison between the tune and chromaticity changes induced by the two dynamic effects (red) and the allowable beam tolerances (blue) shows in a dramatic manner this influence

## Slide 14: And other effects !
AC loss heat load
Rc  5 
short sample limit
(provisional) conclusion – keep Rc as high as possible !
insulate strands ?

## Slide 15: Current distribution
the strands in a multi-strand cables never carry the same current – why ?
Iop
Iop/N
1- non-uniform properties
2- transposition errors
or field gradients
3- joints and splices

## Slide 16: A simple case
simple situation: two-strands cable with a transposition fault linking a flux 
a field ramp generates parasite supercurrents with long range and long time constant
length L
inductance l (self), m (mutual)
transverse conductance g=2/(RcLp)
transposition fault
Lp

## Slide 17: Field Ramp
symmetry line  dI/dx = 0
strand loop
boundary  I= 0
time
B
current distribution from other origins (joints, Ic)
has similar effects

## Slide 18: Scalings
amplitude of the supercurrents:
time constant:
linear scaling with 1/Rc
linear scaling with L
linear scaling with 1/Rc
quadratic scaling with L
times can be extremely long (hours, days, months, years)
the current is frozen in the strands

## Slide 19: Something strange …
periodic field pattern observed along the length of a HERA dipole magnet …
… appearing in all magnets, on all harmonics (SSC, RHIC, LHC) …

## Slide 20: It’s current distribution !
no current in the magnet
… evolves and decays over time constants of several 100’s to 1000’s seconds…
right after a pre-cycle to Inom and ramp to 0
after 9 hours
after 81 hours
courtesy of T. Schreiner

## Slide 21: Why is it important ?
early current sharing and premature quench
  type-A and type-B behaviour in SSC dipoles
  large ramp-rate dependence and pre-cycle influence in LHC dipoles
Rc> 100 
courtesy P. Pugnat, CERN
time
I

## Slide 22: There is more than HEP…
Ramp-rate limitation (RRL) in fusion magnets
  Japanese Demonstration Poloidal Coil (DPC-U1, DPC-U2) showed catastrophic RRL
  RRL observed in US-DPC above Ilimiting
ramp-time, inversely proportional to dB/dt
quench current
M. Takayasu, et al., IEEE Trans. Appl.
Sup., 3(1), 456-459, 1993
 quench
 no quench

## Slide 23: So what ?
do not make Rc too small (<< 10 )
  AC loss
  quench because of excessive heating
  field distortions
do not make Rc too large (>> 100 )
  (frozen) current cannot re-distribute and can cause premature quenches
Rc ()
1
0.1
10
100
1000
is this all ? NO !

## Slide 24: Decay and Snap-back
snap-back
decay
accelerator operation cycle

## Slide 25: Decay
decay during simulated 10,000 s injection
exponential fit
 = 900 s
long time constant (minutes, hours, days)
resembles suspiciously current distribution

## Slide 26: Snap-back
snap-back fit:
b3 [1-(B-Binj)/B]3
b3= 3.7units
B = 20 mT
snap-back
decay
cubic dependence on field change
resembles suspiciously penetration of a SC filament
Notes: On the other hand the snap-back is a very fast recovery of the original multipole values, taking place in a small field sweep (typically some 10 to 20 mT for the MB dipoles). The agreement with a cubic fit suggests that snap-back may be associated with penetration of de-magnetized filaments.

## Slide 27: History and memory
t
decay and SB depend on the powering history
b3
snapback
I
maximum current
Snapback
Q
the parameters space has in fact many more dimensions:
- flat-top current (energy on previous physics run)
- flat-top time (physics run duration)
- waiting time before injection
- ramp-rates (up, down)
- cycles repetition
- temperature
- quench/no quench …
7-dimensional space… machine reproducibility ???

## Slide 28: One …
Current distribution is not uniform in the cables…
…and changes as a function of time generating a time-variable, alternating field along the strands…
R. Stiening, SSC
R. Wolf, CERN

## Slide 29: … two …
…the field change affects the magnetization of the super-conducting filaments...
-B
+B

## Slide 30: … three …
and the magnetization change averages to a net decrease (rectifying effect) – the decay !

## Slide 31: … et voilà !
The magnetization state is re-established as soon as the background field is increased by the same order of the internal field change in the cable (5 to 30 mT) – the snap-back !
-B
+B

## Slide 32: A demonstration experiment
B
measured
computed
Cu strands
NbTi strand
Courtesy of M. Haverkamp
experiment performed at U. Twente

## Slide 33: Ideas - Degaussing LHC
negligible decay after degaussing…
… but useless for operation (giant 11 units SB)!
OK for injection tests ?
degaussing blip
standard cycle

## Slide 34: Ideas - LHC on the Fly
standard decay and SB
negligible decay and SB…
Continuous ramp at injection:
20 mT in 20 min
… but useless for operation (SPS injection tracking not trivial)

## Slide 35: Conclusions – Part I
many complex effects can be understood using simple electromagnetism and appropriate tools
prediction and control are however a challenge
  a SC magnet is a bit like a weather report
    Mega-multi-variable systems, e.g. 35 M-Rc’s in an LHC dipole
    difficult to model if you do not know where to start from !
  production control only partially available (Ic, Rc, …)
  some effects cannot be avoided, e.g. the inhomogeneous current distribution, decay and SB
extensive measurements are mandatory

## Slide 36: Measure, measure, measure…
multi-MCHF project for the characterization of the LHC magnets
and the operation of the LHC (Multipoles-Factory)

## Slide 37: A Bit of Reality…
Field quality reconstructed from measurements performed in MBP2N1
Plot of homogeneity |B(x,y)-B1|/B1 inside the aperture of the magnet:
    blue  OK (1  10-4)
    green  so, so (5  10-4)
    yellow  Houston, we have a problem (1  10-3)
    red  bye, bye (5  10-3)

## Slide 38: A typical LHC operation cycle
operating current
measured b3

## Slide 39: Sony Playstation III (LHC tracking)
coil of MBP2N1 dipole magnet
operating current
Field homogeneity reconstructed from measurements
Rref = 17 mm

## Slide 40: Is your arm steady ?
… or book your vacations today
hit the cross of a 5 CHF coin…
at 30 km distance…
with a 5 mm thick laser…
shooting at
your back !

## Slide 41: LHC control room, day-1
July 14th 2010
00:00 AM
W LHC
and there are still vacancies in control room !
We will need a bunch of very intelligent guys to operate LHC…
What did he say the b3 change would be in the dipoles ? 2*arcsin(log(exp(-t/)+)…
Er… You mean to control chrominance… chromatography… chromaticity ? Did he say where he would be today ?
He’s not at home ! Did he say… Bahamas … or was it Bermudas ?