## Slide 1: Thermal, hydraulic and electromagnetic modeling of superconducting magnet systems
Luca.Bottura @cern.ch
International Conference on Magnet Technology
July 14 – 19, 2013
The Westin Copley Place
Boston, MA USA

## Slide 2: The (coupled) physics domains
Physics | Phenomena | Time scale
Heat flow | Heat flow from supports and structures Heat flow in the coil winding Heat flow along the wire/tape/cable | 1 s 1 s 100 ms
Fluid-dynamics | Proximity cryogenics and refrigeration Coolant steady and transient flow in magnets Coolant steady and transient flow in cables | 100 s 1 s 1 ms
Electro-magnetics | Steady and transient coil currents Steady and transient magnetic fields Current distribution in the wires/tapes/cable Steady and transient Magnetization | 1 s 1 s 1 ms 10ms
Mechanics | Structure mechanics and coil support Coil mechanics under thermal and e.m. loads Cable mechanics Microscopic mechanics | 1 s 1 s 1 ms 100 ms

## Slide 3: How to attack the problem ?
Different physics domains are strongly coupled on comparable time scales
We can imagine a set of building bricks (LEGO), each dedicated to a given “domain”
Geometric proximity (space domains) and difference of characteristic times (time scale domain) are suitable principles to decompose the domains in simpler bricks
  Note: a splitting in physics domain does not necessary yield an easier solution

## Slide 4: The (coupled) physics domains
Cable
Conduction
Cryogenics
Circuits
Magnetics
Physics | Phenomena | Time scale
Heat flow | Heat flow from supports and structures Heat flow in the coil winding Heat flow along the wire/tape/cable | 1 s 1 s 100 ms
Fluid-dynamics | Proximity cryogenics and refrigeration Coolant steady and transient flow in magnets Coolant steady and transient flow in cables | 100 s 1 s 1 ms
Electro-magnetics | Steady and transient coil currents Steady and transient magnetic fields Current distribution in the wires/tapes/cable Steady and transient Magnetization | 1 s 1 s 1 ms 10ms
Mechanics | Structure mechanics and coil support Coil mechanics under thermal and e.m. loads Cable mechanics Microscopic mechanics | 1 s 1 s 1 ms 100 ms

## Slide 5: Cable LEGO

## Slide 6: Cable models – CICC’s
Initial work (1970…1990) was mostly devoted to the helium state and flow, when it was recognized that much of the cable performance depended on cooling
Only later (1990…2000) significant work moved to including self-consistent current distribution and redistribution
The most advanced cable models can solve for
  Conductor temperature (trivial: parabolic, self-adjoint problem, optimal numerical techniques exist)
  Coolant state and flow (tough: hyperbolic system of PDE, no optimal numerical scheme exist)
  Current distribution (tricky: basic equations can be written in different manners, requiring different schemes)

## Slide 7: A bit of pre-history: 1970-1980
First models (known to me): Lee [Lee-1978], Hoffer [Hof-1979], simplified form of the flow equations (no inertia)
Junghans [Jun-1983] (LONSA) further exploits simplified model
Benkowitsch [Ben-1979] validates compressible flow model for supercritical helium (YAQHEL)
Arp [Arp-1980] manipulates flow equations, and produces a code adequate for stability and quench analysis, later used extensively at MIT, NET, and appearing in various instances (clones and mutations) at later times
Downstream propagation only ?!?
[Hof-1979]
Two-sided propagation
[Aga-1987]

## Slide 8: Flourishing of models: 1980-2000
1980
2000
1990
  1991: Wong, stability analysis of US-DPC CICC [Won-1991]
  1991: Dual stability simulations [Kam-1991]
  1994: Martinez studies CICC with central channel [Mar-1994]
  1994: Shajii’s quench theory and QUENCHER [Sha-1994]
1992: Saruman [Bot-1992]
  1983: Marinucci [Mar-1983], in collaboration with Hilal [Mar-1979], develops models for stability (FOCS) and quench (QUBIG)
1983: LONSA [Jun-1983]
1979: YAQHEL [Ben-1979]
[Arp-1980]
1996: Gandalf [Bot-1996]
2000: THEA [Bot-2000]
1996: Koizumi develops quasi-2-D model (POCHI/POCHI2)[Koi-1996]
1994…2000: Vincenta [Sha-xxxx]
1995: Mythrandir [Zan-1995]
  1987: Agatsuma, using a clone of Arp’s code [Aga-1987]
  1985: Quench propagation simulations by Cornelissen [Cor-1985], identify THQB
  1989: Sekiya develops fast quench model [Sek-1989]
[Tad-1989]
  1989: Luongo simulates THQB HEDUMP [Luo-1989]
understand
code
add features

## Slide 9: To conserve or not to conserve ?
The use of conservative form equations is (nearly) a religious dogma in CFD (mandatory
for high-speed flow, shock propagation,…)
Down-side: conservative variables are not convenient for coupled multi-physics problems
  Low-Mach flows are driven by pressure, and they exhibit no shocks
  The exchange of heat between “coolant” and “cooled” is governed by temperature difference
Thou shalt preserve all physically conserved quantities through your numerical scheme
No need to conserve !

## Slide 10: Seminal work of V. Arp
  A complete and exact set of equations for a 1-D flow of a compressible fluid (helium) in non-conservative form
V.D. Arp, Stability and Thermal Quenches in Force-Cooled Superconducting Cables, 1980 Superconducting MHD Magnet Design Conference, MIT, pp. 142-157, 1980
V.D. Arp, Forced Flow, Single-Phase Helium Cooling Systems, Adv. Cryo. Eng.ng, 17, pp. 342-351, 1972
V.D. Arp, Thermodynamics of Single-Phase One Dimensional Fluid Flow, Cryogenics, 15, 285, 1975
Quench initiation and propagation in a force-flow cooled conductor

## Slide 11: CFL condition
CFL condition for stability (Courant, Friedrichs, Lewy, 1928)
Can be grossly violated by using p as primary variable, still maintaining a physical solution (albeit inaccurate at the CFL time scale)
CFL >1
CFL<1
CFL = 0.1
CFL = 1000
DtCFLtrans ≈ 10ms
CFLtrans
CFLlong
(p,v,T) simulation of pressure wave
(p,v,T) form makes ITER quench simulation possible

## Slide 12: Current distribution models
Current distribution in cables can be treated in different ways:
  Network models, well adapted to cables where contacts are localised (e.g. cross contacts)
  Differential equation models, suited for cables where contacts are distributed over the legth (e.g. line contacts)
  Continuum electromagnetics, a non-isotropic solid description of a cable that can be reduced to a system of PDE in 2D or 3D (NOTE: connection to differential forms on manifolds, very active field of research)
None of the above is necessarily the “best”

## Slide 13: Network models
A cable is represented by “sticks” forming a lumped-parameter network of inductances and (non-linear) resistances
  Twente University [Nie-1993]
  SSC work [Akh-1994]
  CUDI [Ver-2006]
  Jackpot [Laa-2010]
Final equation:
L dI/dt +R I = V
Limited to short cable lengths

## Slide 14: Continuum models
The current distribution is described ty differential equations as used in the analysis of transmission lines
  Turck (1974), Schermer (1980), Ries (1980), …
  Krempaski and Schmidt [Kre-1995]
  Bottura, Breschi, Fabbri [Bot-2002]
  THEA [Bot-2000]
  THELMA [Zan-2005]
Final equation:
g l di/dt +r d2i /dx2 + g r i = g v
Requires continuum (non-singular) contact functions

## Slide 15: State-of-the-art in cable models
Arbitrary number of cable solid components that can carry current and transport heat
Arbitrary number of cooling channels
Unlimited range of modeling (no approximations) and operating conditions (wide-range material properties)
Error control and adaptive solver (time and space)
Manageable
THEA [Bot-2000], THELMA [Zan-2005]

## Slide 16: Cryogenic LEGO

## Slide 17: Cryogenic models
Bob-the-builder
  FLOWER: initiated as a boundary condition simulator, evolved in an autonomous network simulator [Bot-2003]
  VINCENTA/VENECIA: a proximity cryogenic simulator is the basic engine of the analysis package [Ven-2013]
ADE S/W
  Modelica/ThermoPower: Equation-based modelling package, assemble components from a library adapted for He [Sav-2010]
  EcosimPro: DAE solver, specific libraries developed at CERN [Bra-2013]
An equivalent hydraulic network consisting of nodes (volumes) and interconnecting components (pipes, valves, pumps, …) largely inspired by nuclear and oil/gas piping process simulation softwares
Two posible approaches:

## Slide 18: Cryogenic models – features and issues
Cryogenic fluids require adjustment w/r to standard process simulators in order to describe the relevant phenomena
  Phase change and separation are crucial to refrigeration
  Helium physics (e.g. He-II) is much different from that of gas, oil or water
Equations describing dynamics are of various and different nature (A, ODE, PDE):
Fast, flexible and generic solver for Algebraic and Differential Equations is mandatory to manage real-size systems

## Slide 19: Heat conduction LEGO

## Slide 20: Heat conduction models
The challenge is to find a suitable and stable interface for coupling (cross-systems ?)
Trivial mathematical problem
  parabolic system of PDE
  FE is optimal for the solution
  Time algorithm well established
A (large) number of commercial S/W are available for the solution of heat transfer in non-linear, non-isotropic media
A (large) number of open-source S/W are similarly available

## Slide 21: Stability of coupling
Coupling heat conduction domains explicitly is subjected to stability conditions on the maximum allowable time step
Small heat capacity and large thermal conductance require small time steps for the stability of the coupling
T1
T2
ph
ArC
ArC
ArC dT1/dt = ph (T2-T1)
ArC dT2/dt = ph (T1-T2)
Dt ≤ ArC / ph

## Slide 22: Current and field LEGO

## Slide 23: Circuit models and magnetic fields
A wealth of models and codes are available for the simulation of
  Current transients in a circuit made by an arbitrary number of inductances, resistances (capacitances, current and voltage sources, passive and active non-linear components, …)
  Magnetic field generated by arbitrary current distributions in space (steady state and transient, in presence of magnetic materials, …)
Consistent modelling is important, e.g.
  current waveform in case of quench with no dump
  AC-loss induced quenchback
Coupling is “easy”, as the time scales of the circuit response are naturally long (large inductances, and small resistances)

## Slide 24: Putting it all together

## Slide 25: MAGS [Mey-1993], [Pas-2003]
In a world of dynosaurs

## Slide 26: MAGS description
Several independent modules
              Winding pack temperature (HEAT3D)
              Inductances and field (EFFI)
              Cable AC loss (EDDY)
              Circuit analysis (MSCAP)
              Quench resistance and power (OHM)
              He dynamics (GANDALF)
              He flow in the manifolds (LINKUP)
Execution sequence is created using a meta-language (similar to FORTRAN DO loops)
Modules are communicating through a shared memory area (managed by a system dependent communication language)

## Slide 27: Saruman [Bot-1994]/Gandalf [Bot-1996]
A little fun

## Slide 28: SARUMAN/GANDALF description
The cable simulator is the main engine, calling the hydraulic and electric network solvers as FORTRAN SUBROUTINES
Monolithic code, compiled all at once and static
SARUMAN/GANDALF
Time stepping loop
do while(t<tend)
...
System solution
...
enddo
FLOWER
POWER
Call Flower()
Call Power()

## Slide 29: VINCENTA/VENECIA [Ven-2013]
Heavy duty stuff

## Slide 30: VINCENTA/VENECIA description
VINCENTA recently evolved into VENECIA
                Core centered around coolant flow in channels, with or without wall
                Additional models for valves, pumps, collectors,… provide the hydraulic network
                Heat conduction is solved in 2-D cross sections
                The system of PDE is solved by FD in time and space
Monolithic code written in FORTRAN (integrally ?) allows access to all bits and pieces (but complex !)

## Slide 31: TEXTO [Nic-2010]
Some pedalling work

## Slide 32: TEXTO description
Couple a number of codes, either on- or off-line, mainly centered on cable simulation
  Cable thermo-hydraulics (GANDALF)
  Heat conduction (ANSYS) (CAST3M attempted)
  Field and AC loss calculation (TRAPS)
  Nuclear heating (MNCP4-C)

## Slide 33: 4C [Sav-2010]
Complicacy

## Slide 34: 4C description
Several S/W modules run separately to solve a specific domain
  Cable and He flow in pipes: M&M
  Proximity cryogenics: ThermoPower (Modelica)
  Heat transfer in solids: Freefem++
Modules are connected by TISC (TLK Inter Software Connector) to allow communication and sync (under Dymola)
T-distribution during a ITER plasma pulse [Sav-2010]

## Slide 35: SuperMagnet [Bot-2007]
Possibilities…

## Slide 36: SuperMagnet description
Building blocks, augmented by a unified interface for data exchange
  THEA
  FLOWER
  POWER
  HEATER
Process and data manager supervises processes
  Data communication based on file system
  Synchronization based on UNIX signals
Naturally parallel on a multi-core machine

## Slide 37: Other (relevant) models
Quench (Wilson), QLASA (Sorbi), TUT (Stenwall)
Gavrilin [Gav-1992]: 3-D solenoid quench simulation code, including
Eyssa [Eys-1995][Eys-1997]: coupled solenoid quench analysis code
ROXIE [Rus-1993]: interactive code, centered on accelerator magnet design and magnetic optimization, augmented by AC loss and quench models
OPERA-QUENCH [OPE-xxxx]: additional module in the Cobham magnet design and analysis code for integrated 3-D quench analysis

## Slide 38: Example: SM analysis of ITER coils
ITER CS, PF, and TF analyed through nominal plasma pulses
Comparison to VINCENTA, mainly from F. Gauthier (ITER-IO)
TF
PF
CS

## Slide 39: HEATER model of TF
163706 nodes
151268 elements
38544 edges
32 sections
mesh generated with ANSYS by F. Gauthier (ITER-IO)

## Slide 40: HEATER model of TF
Different type of elements can be mixed in the winding cross section to describe the geometry features
mesh generated with ANSYS by F. Gauthier (ITER-IO)

## Slide 41: FLOWER model for the TF
TF winding pack cooling
TF structure cooling
132 junctions
25 volumes

## Slide 42: TF temperatures
Pancake 1
Pancake 2
Pancake 7
inlet
outlet
Periodic structure of heat input
Difference in residence times

## Slide 43: TF electric field
Pancake 1
Pancake 2
Pancake 7
Periodic structure of magnetic field
Non-negligible Joule heat
0.3 W
0.4 W
0.4 W

## Slide 44: Comparison to other simulators
PF6 temperature
PF6 pressure
CS2 temperature
Direct comparison to VINCENTA provides a satisfactory match when the models have identical inputs (same physics – sometimes not desireable !!!)
Temperature margins well within allowables

## Slide 45: Example: SM 11 T dipole quench
1…9
10…17
18..20
21,22
1…16
17…34
Conductor
40 Nb3Sn strands
14.7 mm x 1.25 mm
0.1 mm insulation
ANb3Sn = 7.2 mm2
ACu = 8.2 mm2
Aepoxy-glass = 5.5 mm2
6 blocks coil
2 layers/pole
56 turns
Outer layer
Inner layer
Heater

## Slide 46: Simulation
Quench initiation and protection
  INZ in the first turn, mid-plane, 10 cm length
  Quench detection at 50 mV (5 ms integration time)
  OL quench heaters on/off (10 ms delay)
  Self-dump (constant inductance, non-linear resistance)
1-D mesh of cable
  5000 elements (HARD nodes)
  Initial refined region (1 m, 100 elements) around the IHZ
  Adaptive refinement, (1 mm minimum element size, 0.1 m maximum mesh size)
1 THEA process (coil), 1 POWER process (circuit)
condition | 1D/3D | adaptivity | QH | CPU time
Single conductor | 1D | No | No | 654
Single conductor | 1D | yes | No | 867
Coil | 3D | Yes | No | 1702
Coil | 3D | Yes | OL | 1042
Coil | 3D | Yes | OL+IL | 373
MacBook Pro, 2.4 GHz, 4 cores, 16 GB

## Slide 47: Quench propagation and adaptivity
30 m/s
Adaptive mesh tracking fronts
600 m/s
Adaptive mesh: minimum element size 1 mm
Static mesh: 100 mm
Adaptive mesh tracking is a must for practical quench simulation

## Slide 48: Quench heaters and multiple fronts
10 ms
Quench temperature peaks
Mesh density at fronts
20 ms
Heater induced quench
Mesh adapts at single heater quench front
More fronts
40 ms
quench fronts collapse
First block quenches

## Slide 49: Summary results
Current decay during quench
Temperature rise at the hot-spot
Optimistic assumptions (5 ms detection, 10 ms quench heater delay) still yield marginal results at this current density (≈650 A/mm2) and energy density (≈100 MJ/m3)

## Slide 50: Summary
We have come a long way, and the most complex situations can be modeled in a consistent and very pleasant manner through all relevant scales
It is now time to consolidate
  Execution speed
  Modeling flexibility and simplicity
Open technical issues
  Coupling of thermal fields for fast thermal transients
  Geometry/topology pre-processing
  Results post-processing
Looking forward to the next CHATS-AS workshop (Boston, October 2013) for a further iteration on computational physics for applied superconductivity !

## Slide 51: References
[Lee-1978] A.Y. Lee, Adv. Cryo. Eng., 23, 235, 1978.
[Hof-1979] J.K. Hoffer, IEEE Trans. Mag., 15, 331, 1979.
[Ben-1979] J. Benkowitsch, KfK Report 2813, 1979.
[Mar-1979] C. Marinucci, M.A. Hilal, et al. Proc 8th Symp Eng Prob Fusion Res IEEE 79CH141-5 NPS, 1424, 1979.
[Arp-1980] 1980 Superconducting MHD Magnet Design Conference, MIT, 142-157, 1980.
[Jun-1983] D. Junghans, Cryogenics, 23, 220-216, 1983.
[Mar-1983] C. Marinucci, Cryogenics, 23, 579-586, 1983.
[Cor-1985] M.C.M. Cornelissen, C.J. Hoogendoorn, Cryogenics, 25, 185-193, 1985
[Aga-1987] K. Agatsuma, IEEE Trans. Mag., 23(2), 1543, 1987.
[Sek-1989] S. Sekiya, Cryogenics, 29, 25-30, 1989.
[Tad-1989] E. Tada, Cryogenics, 29, 830-840, 1989.
[Won-1989] R.L. Wong, IEEE Proc. SOFE, 1134-1137, 1989.
[Luo-1989] C.A. Luongo, IEEE Trans Mag 25(2), 1589–1595, 1989.
[Kam-1991] A. Kamitani, Cryogenics, 31, 110-118, 1991.
[Bot-1992] L. Bottura, Cryogenics, 32, 659, 1992.
[Gav-1992] A. Gavrilin, Cryogenics, 32, 390-393, 1992.
[Mey-1993] R. Meyber, J. Fus. Energy, 12 (1-2), 99-105, 1993
[Nie-1993] Niessen, E.M.J., Continuum electromagnetics of composite superconductors, PhD thesis, University of Twente, The Netherlands, 1993.
[Rus-1993] S. Russenschuck, ROXIE - the routine for the optimization of magnet X-sections, inverse field computation and coil end design, CERN-LHC-Note-238, 1993
[Sha-1994] A. Shajii, J. Freidberg, J. Appl. Phys., 76(5), 3149, 1994.
[Mar-1994] A. Martinez, Cryogenics, 34, 591-594, 1994.
[Bot-1994] L. Bottura, IEEE Trans. Mag., 30(4), 1978-1981, 1994.
[Akh-1994] A. Akhmetov, et al., J. Appl. Phys. 75, 3176, 1994.
[Kre-1995] L. Krempasky, C. Schmidt, Jour. Appl. Phys., 78 (9), 5800-5810, 1995.
[Eys-1995] Y.M. Eyssa, D. Markiewicz, IEEE TAS 5(2), 487-490, 1995.
[Zan-1995] R. Zanino, S. DePalo, L. Bottura J Fus Energy, 14, 25-40, 1995.
[Bot-1996] L. Bottura, J. Comp. Phys., 125, 26-41, 1996.
[Koi-1996] N. Koizumi, Cryogenics, 36(9), 649-659, 1996.
[Eys-1997] Y.M. Eyssa, IEEE TAS 7(2), 159-162, 1997
[Bot-1999] L. Bottura, C. Rosso, Int J Numer Meth Fluid,s 30,1091–108, 1999.
[Bot-2000] L. Bottura, C. Rosso, M. Breschi, Cryogenics, 40(8–10), 617–626. 2000.
[Bot-2002] L. Bottura, M. Breschi, M. Fabbri, J. Appl. Phys. 92, 7571, 2002.
[Bot-2003] L. Bottura, C. Rosso, Cryogenics, 43, 215-223, 2003.
[Zan-2005] R. Zanino, et al., Fus. Eng. Des., 75-79, 23-27, 2005
[Ver-2006] A. Verweij, Cryogenics, 46, 619-626, 2006
[Ger-2006] J.M. Gery, Modeling The Quench Process in Super-conducting Coils, presentation at CHATS-2006, unpublished.
[Bot-2007] SuperMagnet. User’s Guide. CryoSoft, Ver. 1.0; 2007.
[Sav-2010] L. Savoldi, Cryogenics, 50, 167–176, 2010.
[Laa-2010] E.P.A. van Lanen, A. Nijhuis, Cryogenics, 50, 139–148, 2010.
[Nic-2010] S. Nicollet, Cryogenics, 50, 18–27, 2010.
[Bra-2013] B. Bradu, Cryogenics, 53, 45–50, 2013.
[Ven-2013] http://www.alphysica.com/index.php/venecia.html