## Slide 1: Quench and Protection
Luca.Bottura@cern.ch
Short Course on Superconducting Magnet Design
August 4th, 2002, Houston, TX

## Slide 2: What is a quench ?
quench
heat generation >
heat removal
no
yes
transition to normal state and Joule heat generation in current sharing
temperature increase
stable operating condition
external energy input:
flux jump
conductor motions
insulation cracks
AC loss
heat leaks
nuclear
…
stable operating condition
quench analysis
and protection

## Slide 3: Why is it a problem ?
the magnetic energy stored in the field:
is converted to heat through Joule heating RI2. If this process happened uniformly in the winding pack:
    Cu melting temperature 1356 K
    correspondingEm=5.2 109 J/m3
limit would be Bmax  115 T: NO PROBLEM !
BUT
the process does not happen uniformly (as little as 1 % of mass can absorb total energy)
L
R

## Slide 4: Plan of the lecture
local heating (hot-spot)
normal zone propagation
(heating induced flow)
voltage development
quench detection
safety discharge
yes
heat generation >
heat removal
no
transition to normal state and Joule heat generation in current sharing
temperature increase
stable operating condition
external energy input:
flux jump
conductor motions
insulation cracks
AC loss
heat leaks
nuclear
…
stable operating condition
quench
LTS magnets, adiabatic,
indirect, stagnant or
force-flow helium cooled

## Slide 5: Plan of the lecture
local heating (hot spot)
  Z function
normal zone propagation
  bath-cooled superconductors
  force-flow cooled superconductors (CICC’s)
resistance development
quench protection
  detection
  safety discharge
  quench voltage

## Slide 6: Hot-spot
the quench starts in a point and propagates with a quench propagation velocity
the initial point will be the hot spot at temperature Tmax
Tmax must be limited to:
  limit thermal stresses (see graph)
  avoid material damage (e.g. resins have typical Tcure 100…200 °C)
Tmax < 100 K for
negligible effect
Tmax < 300 K for highly
supported coils
(e.g. accelerator magnets)

## Slide 7: Heat balance during quench

## Slide 8: Material properties
large variation over the range of interest !
copper resistivity as f(RRR)
copper specific heat

## Slide 9: Adiabatic hot spot temperature
adiabatic conditions at the hot spot :
can be integrated:
cable operating current density
stabilizer fraction
total volumetric heat capacity
stabilizer resistivity
remember:
B.J. Maddock, G.B. James, Proc. IEE, 115 (4), 543, 1968

## Slide 10: Plan of the lecture
local heating (hot spot)
  Z function
normal zone propagation
  bath-cooled superconductors
  force-flow cooled superconductors (CICC’s)
resistance development
quench protection
  detection
  safety discharge
  quench voltage

## Slide 11: The Z(Tmax) function
the function Z(Tmax) is a cable property:
the volumetric heat capacity C is defined using the material fractions fi:
Z(Tmax) can be computed (universal function) for a given cable design (i.e. fi fixed) !

## Slide 12: Z(Tmax) for pure materials
assuming the cable as being made of stabilizer (good approximation):
  fst = 1,
  C = stcst
Z(Tmax) is a material property that can be tabulated:
Copper at B=0 T

## Slide 13: How to limit Tmax
implicit relation between Tmax , fst , Jop , decay
to decrease Tmax
    reduce operating current density (Jop)
    discharge quickly (decay )
    add stabilizer (fst)
    choose a material with large Z(Tmax) 
stabilizer material property
electrical operation of the coil (energy, voltage)
cable fractions design

## Slide 14: Z(Tmax) for typical stabilizers
Tmax100 K

## Slide 15: Tmax calculation issues
other materials in the cable affect the value of Tmax
  structures (e.g. steel jacket in CICC’s)
  cable insulation in close proximity
  temperature gradients in the cable are difficult to estimate, and to take into account in Z(Tmax)
effect of heat transfer
  inter-turn heat transfer – small effect because of insulation
  heat transfer to helium – major effect for T<10 K, not so important afterwards
additional heat capacity and heat transfer generally make the temperature lower
  the adiabatic calculation is conservative and a good method for design, small corrections can be applied

## Slide 16: What are MIITs ?
sometimes (HEP accelerator and detector magnets) the energy balance is written as follows:
the r.h.s is measured in
Mega I  I vs. Time (MIITs)
however, now the l.h.s. is no longer a material property (depends on cable)

## Slide 17: Plan of the lecture
local heating (hot spot)
  Z function
normal zone propagation
  bath-cooled superconductors
  force-flow cooled superconductors (CICC’s)
resistance development
quench protection
  detection
  safety discharge
  quench voltage

## Slide 18: Quench propagation (bath-cooled magnets)
x
vquench
TJ
Teq
Top
T
xquench
q’’’J =q’’’Jmax
q’’’J =0
T
Tcs
Top
Tc
TJ
fixed reference frame
moving reference frame

## Slide 19: Quench propagation (bath-cooled magnets)
T
Tcs
Top
Tc
TJ
recovery
propagation
Maddock equal area
cryostable
for constant properties (, k, C)

## Slide 20: Turn-to-turn propagation
Heat conduction spreads the quench from turn to turn as it plods happily along a conductor at speed vlongitudinal. The vtransverse is approximated as:
insulation conductivity
(large) correction factors for geometry, heat capacity, non-linear material properties apply to the scaling !
conductor in normal state
insulation

## Slide 21: Plan of the lecture
local heating (hot spot)
  Z function
normal zone propagation
  bath-cooled superconductors
  force-flow cooled superconductors (CICC’s)
resistance development
quench protection
  detection
  safety discharge
  quench voltage

## Slide 22: Quench propagation (force-flow-cooled magnets)
the helium is heated in the normal zone and expands (d/dT < 0)
    pressure increase
    heating induced massflow of hot helium
x
vquench
TJ
Tcable
Top
T
xquench
q’’’Jmax
q’’’J =0
vhelium
Thelium
vquench > vhelium
vquench = vhelium
vquench < vhelium
???

## Slide 23: Dresner’s helium bubble
Dresner’s postulate:
    …the velocity of the normal zone propagation equals the local velocity of expansion of helium.
consequence:
    …the normal zone engulfs no new helium, or in oth words that the heated helium comprises only the atoms originally present in the initial normal zone. We are thus led to the picture of a bubble of hot helium expanding against confinement by the cold helium on either side of it.
OK if h is large and cable conduction is small
L. Dresner, Proc. 11th Symp. Fus. Eng.ng, 1218, 1985
L. Dresner, Proc. 10th Symp. Fus. Eng.ng, 2040, 1983
vhelium
vquench
vhelium
vquench

## Slide 24: Shajii’s universe of quench
quenched
length
quench
intensity
A. Shajii, J. Freidberg, J. Appl. Phys., 76 (5), 477-482
normalization

## Slide 25: Pressure rise
maximum pressure during quench for:
  full length normal
  constant heating rate
conduit thickness and diameter of venting lines must be sized accordingly !
J.R. Miller, L. Dresner, J.W. Lue, S.S. Shen, H.T. Yeh, Proc. ICEC-8, 321, 1980

## Slide 26: Recap
the quench propagates in the coil at speed vquench longitudinally (vlongitudinal) and transversely (vtransverse)…
…the total resistance of the normal zone Rquench(t) grows in time following
    the temperature increase, and
    the normal zone evolution…
…a resistive voltage Vquench(t) appears along the normal zone…
…that dissipates the magnetic energy stored in the field, thus leading to a discharge of the system in a time decay.
the knowledge of Rquench(t) is mandatory to verify the protection of the magnetic system !

## Slide 27: Plan of the lecture
local heating (hot spot)
  Z function
normal zone propagation
  bath-cooled superconductors
  force-flow cooled superconductors (CICC’s)
resistance development
quench protection
  detection
  safety discharge
  quench voltage

## Slide 28: Quench resistance: 1-D
take:
    short initial normal zone
    constant current I = Iop so that
    maximum temperature as given by:
    1-D quench propagation with vquench = constant
then:
x
vquench
Tmax
T
vquench

## Slide 29: Quench resistance: 3-D
in reality the quench propagates in 3-D !
the resistance growth is computed solving a volume integral:
3-D vs. 1-D
M. Wilson, Superconducting Magnets, Plenum Press, 1983
vlongitudinal
vtransverse

## Slide 30: Quench propagation in reality
matters are (even) more complex:
    a magnet has boundaries (e.g. the inner outer radius of a solenoid)
    the quench can byte its tail as it travels along the conductor
the real Rquench(t) falls then between the 1-D and the 3-D limits, depending on the details of the conductor and winding considered
M. Wilson, Superconducting Magnets, Plenum Press, 1983
art-work by M. Wilson

## Slide 31: Plan of the lecture
local heating (hot spot)
  Z function
normal zone propagation
  bath-cooled superconductors
  force-flow cooled superconductors (CICC’s)
resistance development
quench protection
  detection
  safety discharge
  quench voltage

## Slide 32: Quench protection
What if ½ L I2 > R I2 ?
Balance the initial magnetic energy vs. dissipated resistive power during the discharge:
initial magnetic energy
total dissipated resistive power during decay
yes
no
self-protected:
detect, switch-off power and
let it go… most likely OK
WARNING: the reasoning here is qualitative, conclusions require in any case detailed checking
requires protection:
detect, switch-off power and
do something !

## Slide 33: Plan of the lecture
local heating (hot spot)
  Z function
normal zone propagation
  bath-cooled superconductors
  force-flow cooled superconductors (CICC’s)
resistance development
quench protection
  detection
  safety discharge
  quench voltage

## Slide 34: Quench detection: voltage
a direct quench voltage measurement is subject to inductive pick-up (ripple, ramps)
immunity to inductive voltages (and noise rejection) is achieved by compensation
L
Rquench
L1
L2
Rquench
R1
R2

## Slide 35: Co-wound voltage taps
co-wound (non-inductive) voltage taps are an alternative to achieve compensation
sometimes the voltage tap can be directly inserted in the conductor, thus providing the best possible voltage compensation and noise rejection
Lcoil
Rquench
LV-tap
jacket equipotential with conductor

## Slide 36: Quench detection: indirect
quench antenna’s: variation of magnetization and current distribution in cables generates a voltage pick-up from a magnetic dipole change localised at the quenching cable
optical fibers in cables/coils: variation of fiber refraction index with temperature is detected as a change of the interference pattern of a laser beam traveling along the fiber
pressure gauges and flow-meters: heating induced flow in internally cooled cables is detected at the coil inlet/outlet
co-wound superconducting wires: variation of resistance with temperature can be measured
voltage measurement is still best
the QUELL experiment:
a quench detection test-bed

## Slide 37: Plan of the lecture
local heating (hot spot)
  Z function
normal zone propagation
  bath-cooled superconductors
  force-flow cooled superconductors (CICC’s)
resistance development
quench protection
  detection
  safety discharge
  quench voltage

## Slide 38: Strategy 1: energy dump
the magnetic energy is extracted from the magnet and dissipated in an external resistor:
the integral of the current:
can be made small by:
  fast detection
  fast dump (large Rdump)
B.J. Maddock, G.B. James, Proc. Inst. Electr. Eng., 115, 543, 1968
L
Rquench
Rdump
S
normal operation
quench

## Slide 39: Dump time constant
magnetic energy:
maximum terminal voltage:
dump time constant:
operating current
maximum terminal voltage
interesting alternative:
non-linear Rdump or voltage source
increase Vmax and Iop to achieve fast dump time

## Slide 40: Switches
switching kA’s currents under kV’s of voltage is not easy:
  mechanical interrupters
  thyristor’s
  Gate Turn-Off thyristor’s
  Insulated Gate Bipolar Transistor’s
  fuses (explosive, water cooled)
  superconducting
cost and reliability are most important !

## Slide 41: Strategy 2: coupled secondary
the magnet is coupled inductively to a secondary that absorbs and dissipates a part of the magnetic energy
advantages:
  magnetic energy partially dissipated in Rs (lower Tmax)
  lower effective magnet inductance (lower voltage)
  heating of Rs can be used to speed-up quench propagation (quench-back)
disadvantages:
  induced currents (and dissipation) during ramps
L
Rquench
Rdump
S
Ls
Rs
normal operation
M
quench

## Slide 42: Strategy 3: subdivision
the magnet is divided in sections, with each section shunted by an alternative path (resistance) for the current in case of quench
advantages:
  passive
  only a fraction of the magnetic energy is dissipated in a module (lower Tmax)
  transient current and dissipation can be used to speed-up quench propagation (quench-back)
disadvantages:
  induced currents (and dissipation) during ramps
P.F. Smith, Rev. Sci. Instrum., 34 (4), 368, 1963.
L1
R1
L2
R2
L3
R3
heater
normal operation
quench
charge

## Slide 43: Tmax in subdivided system
in a subdivided system the energy dumped in each section is reduced because of
    the resistive bypass
    inductive coupling, reducing the effective inductance of each section:
the hot spot temperature scales as:
P.F. Smith, Rev. Sci. Instrum., 34 (4), 368, 1963.
ratio of TmaxN in a system subdivided in N sections relative to the Tmax1 in the same system with no subdivision
construction becomes complicated !

## Slide 44: Magnet strings
P.F. Smith, Rev. Sci. Instrum., 34 (4), 368, 1963.
magnet strings (e.g. accelerator magnets, fusion magnetic systems) have exceedingly large stored energy (10’s of GJ):
    energy dump takes very long time (10…100 s)
    the magnet string is subdivided and each magnet is by-passed by a diode (or thyristor)
    the diode acts as a shunt during the discharge
M1
M2
M3
MN

## Slide 45: Strategy 4: heaters
the quench is spread actively by firing heaters embedded in the winding pack, in close vicinity to the conductor
heaters are mandatory in:
  high performance, aggressive, cost-effective and highly optimized magnet designs…
  …when you are really desperate
advantages:
  homogeneous spread of the magnetic energy within the winding pack
disadvantages:
  active
  high voltages at the heater
winding
heater

## Slide 46: Plan of the lecture
local heating (hot spot)
  Z function
normal zone propagation
  bath-cooled superconductors
  force-flow cooled superconductors (CICC’s)
resistance development
quench protection
  detection
  safety discharge
  quench voltage

## Slide 47: Quench voltage
electrical stress can cause serious damage (arcing) to be avoided by proper design:
  insulation material
  insulation thickness
  electric field concentration
REMEMBER: in a quenching coil the maximum voltage is not necessarily at the terminals
the situation in subdivided and inductively coupled systems is complex, may require extensive simulation
Vext
Rquench
Vext
Vquench

## Slide 48: Helium breakdown
during a quench helium undergoes drastic changes in its state (p,T,) that affect its dielectric strength:
= helium density (Kg/m3)
d = gap (mm)
K = 1279
= 0.878
 = 0.901
WATCH-OUT for pool boiling magnets and/or helium leaks
gap that sustains a voltage of 1 kV
liquid
vapour
leak
Vbreakdown in kV

## Slide 49: Summary…
quench protection cannot be (easily) added afterwards
protection is an integral part of the magnet design:
    balance of cost/complexity (e.g. structure, electrical insulation) vs. design margins (e.g. stabilizer fraction)
quenches can and will always happen:
    protection must be reliable and fail-safe
as usual:
“There are more things in heaven and earth, Horatio, than are dreamt of in your philosophy…”

## Slide 50: …and where to find out more
M.N. Wilson, Superconducting Magnets, Plenum Press, 1983.
P.J. Lee ed., Engineering Superconductivity, J. Wiley & Sons, 2001.
B. Seeber ed., Handbook of Applied Superconductivity, IoP, 1998.
Y. Iwasa, Case Studies in Superconducting Magnets, Plenum Press, 1994.

## Slide 51: More topics

## Slide 52: Propagation speed
long coil
high pressure rise
long coil
low pressure rise
short coil
high pressure rise
short coil
low pressure rise

## Slide 53: Examples
MRI magnet protection

## Slide 54: MRI magnet hot spot
Bop = 2 T
Top = 4.2 K
Iop = 400 A
Tmax < 150 K
Jop = 200 A/mm2
fst =0.83, fsc =0.17
Z(150) =10.4 1016 (A2 s/m4)
R 800
2000
NbTi wire
1 mm x 2 mm
Cu:NbTi=5
Jc 5000 A/mm2
RRR=100
Tc = 8.7 K
decay=2 s

## Slide 55: MRI magnet hot spot
the only way to increase Jop is to pay by either:
  increase in maximum allowable temperature (Tmax)
  more stabilizer (fst )
  faster decay (decay )
e.g. accepting Tmax  400 K and decay  1 s the maximum allowable Jop is 377 A/mm2
2 s
377 A/mm2

## Slide 56: MRI magnet quench velocity
Top = 4.2 K
Jop = 200 A/mm2
TJ =8.15 K
st =2.5 10-10 (m)
kst =1000 (W/mK)
Cst =4450 (J/m3K)
kin =0.15 (W/mK)
R 800
2000
NbTi wire
1 mm x 2 mm
Cu:NbTi=5
Jc 5000 A/mm2
RRR=100
Tc = 8.7 K
vlongitudinal=11.3 m/s
vtransverse=0.14 m/s

## Slide 57: MRI magnet quench resistance
Jop = 200 (A/mm2)
fst = 0.83, fsc = 0.17
Ast =1.67 (mm2)
T0 = 150 (K)
st(T0) =7.3 10-9 (m)
Z(T0) =10.4 1016 (A2 s/m4)
vlongitudinal = 11.3 (m/s)
vtransverse = 0.14 (m/s)
1-D
3-D

## Slide 58: MRI magnet self discharge
L=43.2 (H)
Iop = 400 (A)
Em = 3.46 (MJ)
3-D
1-D
1-D
3-D
Pr = 10.9 kW
Pr = 1.94 MW
Er = 5.8 kJ
Er = 692 kJ
we are short of resistive power… what now ???