## Slide 1: AC Losses
Plan
critical state model
flux jumping and fine filaments
hysteresis loss
loss in terms of magnetization
filamentary composites
coupling between filaments in a wire:
- twisting
- time constants - coupled magnetization
- coupling losses
coupling between wires in a cable
self field loss and Norris’ model
HTS materials
Martin Wilson

## Slide 2: The critical state model
when the field sweep stops E  0
superconductor goes back to Jc
- and then stays there
this is the critical state model
within a superconductor, the current density is + Jc - Jc or zero
there's nothing in between!
superconducting slab placed in a changing magnetic field By
assume it's infinitely long in the z and y directions - simplifies the algebra to a 1dim problem in x
increase the external field from zero
B
J
J
x
dB/dt produces an electric field E in the superconductor which drives it into the resistive state
E
J
Jc

## Slide 3: Hysteresis
field induces screening currents
just like eddy currents – try to oppose the field change
unlike eddy currents, do not decay
plot B within slab as external B is raised
in the 1 dim infinite slab geometry, Maxwell's equation says
B
Jc
Jc
fully penetrated
on reducing B, the change in Jc (electric field) comes in from the outer surfaces
Jc
Jc
B
Jc
Jc
Jc
Jc
Jc
Jc
B
Note: the state depends on history - hysteresis

## Slide 4: The flux penetration process
B
field increasing from zero
field decreasing through zero
according to the Bean critical state model
fully penetrated

## Slide 5: The flux penetration process (2)
B
field increasing from zero
field decreasing through zero
according to the Bean critical state model
Remember
current density everywhere is Jc or zero
change comes in from the outer surface

## Slide 6: Flux penetration from another viewpoint
superconductor
vacuum
Think of the screening currents, in terms of a gradient in fluxoid density within the superconductor. Pressure from the increasing external field pushes the fluxoids against the pinning force, and causes them to penetrate, with a characteristic gradient in fluxoid density
At a certain level of field, the gradient of fluxoid density becomes unstable and collapses
– a flux jump

## Slide 7
Flux jumping: why it happens
It arises because:-
magnetic field induces screening currents, flowing at critical density Jc
Unstable behaviour is shown by all type 2 and HT superconductors when subjected to a magnetic field
B
B
* change in screening currents allows flux to move into the superconductor
flux motion dissipates energy
thermal diffusivity in superconductors is low, so energy dissipation causes local temperature rise
critical current density falls with increasing temperature
go to *
Q


Jc
Cure flux jumping by making superconductor in the form of fine filaments – weakens Q

## Slide 8
AC Losses: fully penetrated (large field changes)
although they have no loss in the steady state, all superconductors dissipate energy in changing fields
physically the reason is that changing magnetic field produces an electric field in the superconductor, which drives the current density beyond critical
a
x
dx
B
screening currents induced in slab by external field, consider 'sub slab' at x, width dx
B
external field changes 
change in flux linked between x and electric centre line
energy dissipated within dx (per unit height and length)
total energy dissipated per unit volume of slab
E
J
Jc
- hence fine filaments!

## Slide 9: Magnetization
for cylindrical filaments the inner current boundary is roughly elliptical (controversial)
when fully penetrated, the magnetization is
where a = filament radius
When viewed from outside the sample, the persistent currents produce a magnetic moment. We can thus define a magnetization.
for a fully penetrated slab

## Slide 10: Magnetization of a superconductor
The induced currents produce a magnetic moment and hence a magnetization
= magnetic moment per unit volume
M
Bext

## Slide 11
Magnetization and AC Losses
ac losses are the work done by the external field
if the sample is taken round a closed magnetization loop such that the finishing conditions are the same as the starting conditions it may be shown that the ac loss Q is
= area of magnetization loop
for a proof see any text book on Thermodynamics
M
H
where Q is in Jm-3 and M is in units of H
if the magnetization is small compared to the external field (almost always the case) we may also write

## Slide 12
AC Losses: below penetration (small field changes)
Bp
define penetration field amplitude
for small amplitudes of field oscillation
Bm
where
remark
is like a field energy
Bm
for large amplitudes of field oscillation
in general

## Slide 13
Recap
AC Losses: general formulation
where

## Slide 14: Filamentary composite wires
recap
We can reduce Q by making the superconductor as fine filaments. For ease of handling, an array of many filaments is embedded in a copper matrix
Unfortunately, in changing fields, the filament are coupled together; screening currents go up the LHS filaments and return down the RHS filaments, crossing the copper at each end.
In time these currents decay, but for wires ~ 100m long, the decay time is many years!
So the advantages of subdivision are lost

## Slide 15: Twisting
coupling may be reduced by twisting the wire, because the induced emf reverses every half twist pitch
induced coupling currents then flow along the filaments and then vertically down through the matrix
at each end of the wire, the current crosses over and then returns along the other side of the wire
B`
these current paths encounter resistance in the vertical parts so that the currents decay with a time constant
where t is the transverse resistivity across the wire
the magnetization is increased by a rate dependent component
where B` is the rate of change of field

## Slide 16: Rate dependent magnetization
magnetization of the wire has two components:
2) coupling between filaments
M
B
1) persistent current in filaments
ac loss per cycle is
loss power is
Joules per m3
Watts per m3
3) total magnetization

## Slide 17: Magnetization and field errors
magnetization produces field errors in the magnet
error has two components – persistent current and coupling
skew quadrupole error in Nb3Sn dipole (Universityof Twente)

## Slide 18: Losses in cables
like the filaments in composite wires, the wires in cables must be twisted to reduce coupling
to ensure good current sharing during ramp up to field, the wires should be in electrical contact with each other
this electrical contact means that wires can be coupled together during changing fields
coupling means further increase in magnetization and extra losses
Rutherford cable  used in accelerators
twisted rope 
used in CICCs 

## Slide 19: Rutherford cable: field perpendicular to broad face
changing fields perpendicular to the broad face induce diamond shaped current loops
current flows along the top surface then downwards through a crossover along the bottom surface and then over the edge and up to the top surface
a whole range of different loops are possible and are all induced simultaneously by a changing field
they must be summed together to calculate the magnetization
for exact calculations, a network model should be used
here we use an approximate continuum model, which gives similar answers
B

## Slide 20: Coupling magnetization in Rutherford cable
1) field perpendicular to broad face, coupling through crossover resistance Rc
Ra
Rc
where Rc is crossover resistance per contact and rc is crossover resistance per unit area
2) field perpendicular to broad face, coupling through adjacent resistance Ra
or
where Ra is adjacent resistance per contact and ra is adjacent resistance per unit area
3) field parallel to broad face, coupling through adjacent resistance Ra

## Slide 21: AC loss in cables
in general, for any cable, we may write
where n are the time constants of the coupling currents
fn and gn are shape factors
n is the fraction of cable volume occupied by the coupling current
the ac loss per cycle is
the loss power is
Joules per m3
Watts per m3
Note the resemblance to eddy currents
Beware of filling factors – watts per unit volume of what?
M can also include coupling between filaments in wires

## Slide 22: Self field (transport current) losses
everything far has been about externally applied fields – applies to magnets and magnetic machines, eg transformers etc
conductors carrying a transport current also generate self field
penetration of the self field produces an electric field which produces loss, just like the external field
for a slab, this field is uniform ± on each side of the slab
Jc
Jc
B
B
B
Ic
B
I
for a circular wire, lines of self field are concentric circles, centred on the wire
Note: self field penetrates from the outside - just like external field – critical state model
I < Ic self field not fully penetrated
I = Ic self field fully penetrated

## Slide 23: Penetration of the transport current
B
current increasing from zero
current decreasing through zero
slab according to the Bean critical state model

## Slide 24: AC loss from transport current (self field )
slab self field loss is the same as external field loss below penetration
where
similar calculation for a round wire shows
Bms
Norris theory * is formulated in terms of Ic and loss per unit length of wire
(recap: loss per cycle per unit volume)
Norris also showed that loss per unit length of an elliptical conductor is the same as a round wire, regardless of ellipticity
* ref: W.T. Norris J. Phys. D3 pp489 (1970)

## Slide 25: Transport current loss function
recap: loss per unit length of wire
applies to round and elliptical wires regardless of ellipticity
Norris nomenclature:

## Slide 26: HTS materials
the critical state model only works if there is a steep rise in electric field immediately above Jc
this allows us to say that J is everywhere either Jc or zero
HTS materials have a much 'softer' transition and develop resistance slowly above Jc
thus, when an electric field is present, the current density in HTS can be much higher than Jc - particularly at high ramp rates
ac losses then become a non-linear problem, requiring numerical solution
can utilize commercial eddy current software
softness of the HTS transition gets worse as you approach the irreversibility line
E
J
Jc
HTS
LTS

## Slide 27: Twisting and self field
In filamentary composite wires, self field flux lines link between the inner and outer annuli of filaments
twisting makes no difference
so the self field loss is the same as a solid wire, apart from dilution of Jc
Bself
the same is true of cables if the inner wires do not change places with outer
to reduce self field loss, the cable must be fully transposed, eg Litz wire 

## Slide 28: AC loss: concluding remarks
ac losses can be the dominant heat load (and hence running cost) in pulsed magnets and magnetic machines for electric power applications
calculating losses is a complicated business!
there are many components of loss but, providing no component is too large, we may calculate them separately and add them together
HTS materials are special because of their 'soft' transition  numerical methods
the two basic components of loss are persistent currents within the superconductor (hysteresis) and coupling currents between superconducting filaments (eddy currents)
it is useful always to have in mind that Bm2 / 2o is the maximum loss per cycle available from the field energy ('not too large' above means small compared with Bm2 / 2o )
for low ac loss in changing external fields need
- fine filaments
- tight twist pitch
- resistive matrix
for low ac loss in self field need
- fine wire size
- fully transposed cables

## Slide 29: To learn more: some useful references
'Handbook of Applied Superconductivity', ed B Seeber, all of part B, pub Institute of Physics Publishing 1998 ISBN 0 7503 0377 8.
W.T. Norris J. Phys. D3, pp 489 (1970) and J. Phys. D4, pp 1358 (1971).
'ICMC Topical Conference on AC and Stability in Low and High Tc Superconductors', University of Twente, May 1998, pub North Holland, also in Physica C Vol 310.
Martin N Wilson, 'Superconducting Magnets', pub Oxford 1983, ISBN 0 19 854810 9.
'Electrodynamics of Superconducting Cables in Accelerator Magnets' thesis A.P. Verweij, University of Twente, 1995, ISBN 90 9008555-6.
'A general treatment of ac losses in multifilamentary superconductors', A.M. Campbell, Cryogenics Jan. 1982, pp 3.