## Slide 1: Stability (and Cooling)
Luca.Bottura@cern.ch
Short Course on Superconducting Magnet Design
August 4th, 2002, Houston, TX

## Slide 2: Plan of the lecture
training and degradation
perturbation spectrum overview
heat balance
    Joule heating
    cooling and heat transfer
stability criteria
    enthalpy stabilization
    cryostability
    cold end recovery and the equal-area theorem
    meta-stable conductors:
      well-cooled operation in CICC’s
      MPZ and MQE
focus on LTS magnets, adiabatic, indirect, stagnant or force-flow helium cooled

## Slide 3: Plan of the lecture
training and degradation
perturbation spectrum overview
heat balance
    Joule heating
    cooling and heat transfer
stability criteria
    enthalpy stabilization
    cryostability
    cold end recovery and the equal-area theorem
    meta-stable conductors:
      well-cooled operation in CICC’s
      MPZ and MQE

## Slide 4: Training…
Superconducting solenoids built from NbZr and Nb3Sn in the early 60’s quenched much below the rated current …
… the quench current increased gradually quench after quench: training
M.A.R. LeBlanc, Phys. Rev., 124, 1423, 1961.
NbZr solenoid
Chester, 1967
P.F. Chester, Rep. Prog. Phys., XXX, II, 561, 1967.

## Slide 5: … and degradation
NbZr solenoid vs. wire
Chester, 1967
Ic of NbZr wire
Imax reached in NbZr solenoid
… but did not quite reach the expected maximum current for the superconducting wire !
This was initially explained as a local damage of the wire: degradation, a very misleading name.
All this had to do with stability !
P.F. Chester, Rep. Prog. Phys., XXX, II, 561, 1967.

## Slide 6: Training today
training of an LHC short dipole model at superfluid helium
  still (limited) training may be necessary to reach nominal operating current
  short sample limit is not reached, even after a long training sequence
stability is (still) important !
10 T field in the dipole bore
8.3 field in the dipole bore
Courtesy of A. Siemko, CERN, 2002

## Slide 7: Why training ?
stable operating condition
external energy input:
flux jump
conductor motions
insulation cracks
AC loss
heat leaks
nuclear
…
temperature increase
quench
yes
no
stable operating condition
transition to normal state and Joule heat generation in current sharing
heat generation >
heat removal
stability analysis
and design

## Slide 8: Plan of the lecture
training and degradation
perturbation spectrum overview
heat balance
    Joule heating
    cooling and heat transfer
stability criteria
    enthalpy stabilization
    cryostability
    cold end recovery and the equal-area theorem
    meta-stable conductors:
      well-cooled operation in CICC’s
      MPZ and MQE

## Slide 9: Perturbation spectrum
mechanical events
    wire motion under Lorentz force, micro-slips
    winding deformations
    failures (at insulation bonding, material yeld)
electromagnetic events
    flux-jumps (important for large filaments, old story !)
    AC loss (most magnet types)
    current sharing in cables through distribution/redistribution
thermal events
    current leads, instrumentation wires
    heat leaks through thermal insulation, degraded cooling
nuclear events
    particle showers in particle accelerator magnets
    neutron flux in fusion experiments

## Slide 10: Perturbations
transient (stability concern)
  point Q [Joules]
  distributed Q’’’ [Joules/m3] [mJ/cm3]
continuous (sizing of cooling system)
  point q [Watts]
  distributed q’’’ [Watts/m3]

## Slide 11: Perturbation overview

## Slide 12: Plan of the lecture
training and degradation
perturbation spectrum overview
heat balance
    Joule heating
    cooling and heat transfer
stability criteria
    enthalpy stabilization
    cryostability
    cold end recovery and the equal-area theorem
    meta-stable conductors:
      well-cooled operation in CICC’s
      MPZ and MQE

## Slide 13: Heat balance

## Slide 14: Temperature transient
heat pulse…
…effect of heat conduction and cooling…
Q’’’ext = Q’’’+
generation
>
cooling
Q’’’ext = Q’’’-
generation
<
cooling

## Slide 15: Energy margin
Q’’’, energy margin
  minimum energy density that leads to a quench
  maximum energy density that can be tolerated by a superconductor, still resulting in recovery
    simple and experimentally measurable quantity (…)
    measured in [mJ/cm3] for convenience (values  1…1000)
    also called stability margin
    compared to the energy spectrum to achieve stable design
Q, quench energy
    better adapted for disturbances of limited space extension
    measured in [J] to [mJ]

## Slide 16: Plan of the lecture
training and degradation
perturbation spectrum overview
heat balance
    Joule heating
    cooling and heat transfer
stability criteria
    enthalpy stabilization
    cryostability
    cold end recovery and the equal-area theorem
    meta-stable conductors:
      well-cooled operation in CICC’s
      MPZ and MQE

## Slide 17: Critical surface Jc(B,T)
T
Jc
B
14.5 T
9 K
typical NbTi
5 T
4.2 K
3000 A/mm2
operating plane
J
B
Jop
Bop
Bc
Bmax
Jc
current margin
temperature margin
Tcs
J
T
Jop
Top
Tc
Jc

## Slide 18: V-I characteristic
NbTi: normal  6.5 10-7 m
Cu, Al:   10-11…10-10 m
ideal…
…and real
resistive dissipation:
Joule heat

## Slide 19: Current sharing
Tcs
T
Iop
Top
Tc
Ic
Tcs < T < Tc
T < Tcs
T > Tc
quenched
curent sharing
stabilizer
superconductor

## Slide 20: Joule heating
T
Tcs
Top
Tc
Iop
current in stabilizer
current in superconductor

## Slide 21: Joule heating (cont’d)
linear approximation for Jc(T)
Joule heating
Iop
T
Tcs
Top
Tc

## Slide 22: Plan of the lecture
training and degradation
perturbation spectrum overview
heat balance
    Joule heating
    cooling and heat transfer
stability criteria
    enthalpy stabilization
    cryostability
    cold end recovery and the equal-area theorem
    meta-stable conductors:
      well-cooled operation in CICC’s
      MPZ and MQE

## Slide 23: Cooling modes (low-Tc)
indirect
    contact to a heat sink through conduction (cryoplant, cryocooler)
    in practice  no cooling on the time scale of interest for stability
bath cooling
    pool of liquid helium at atmospheric pressure and saturation temperature (4.2 K)
    boiling heat transfer
force-flow cooling
    supercritical or two-phase flow, warm or cold circulation
superfluid cooling
    stagnant bath, heat removal through counterflow heat exchange

## Slide 24: Helium phase diagram
forced-flow
pool-boiling
sub-cooled
superfluid
Best to take the cryogenics course !

## Slide 25: Boiling heat transfer
nucleate boiling heat flux:
q’’  (Ts-The)n1
n1  2…3
PNBF  10 kW/m2
film boiling heat flux:
q’’  (Ts-The)

## Slide 26: Heat transfer coefficient

## Slide 27: Plan of the lecture
training and degradation
perturbation spectrum overview
heat balance
    Joule heating
    cooling and heat transfer
stability criteria
    enthalpy stabilization
    cryostability
    cold end recovery and the equal-area theorem
    meta-stable conductors:
      well-cooled operation in CICC’s
      MPZ and MQE

## Slide 28: Adiabatic stability
adiabatic conditions:
    no cooling (dry or impregnated windings)
    energy perturbation over large volume (no conduction)
stable only if q’’’Joule=0 (TTcs) ! Integrate:
energy margin
volumetric enthalpy

## Slide 29: Low temperature heat capacity
Note that C  0 for T  0 !

## Slide 30: Specific enthalpy
2
30
2
3
enthalpy reserve increases at increasing T
do not sub-cool !
(if you can only avoid it…)

## Slide 31: Adiabatic stabilization
NbTi
Tc0  9.5 K
Bc20  14.5 T
Nb3Sn
Tc0  18 K
Bc20  28 T
fsc=0.3, fst=0.4, fin=0.3
for a typical winding

## Slide 32: Adiabatic stabilization
Nb3Sn
sub-cooling makes sense only
above  8 T for NbTi and  15 T for Nb3Sn
NbTi
4.2 K
1.8 K

## Slide 33: Plan of the lecture
training and degradation
perturbation spectrum overview
heat balance
    Joule heating
    cooling and heat transfer
stability criteria
    enthalpy stabilization
    cryostability
    cold end recovery and the equal-area theorem
    meta-stable conductors:
      well-cooled operation in CICC’s
      MPZ and MQE

## Slide 34: Cryostability
cooling in a bath of pool boiling helium
    ignore conduction for large energy perturbations
request steady state stability in all conditions:
worst possible case
generation
cooling
A.R. Krantowitz, Z.J.J. Stekly, Appl. Phys. Lett., 6, 3, 56-57, 1965.
Z.J.J. Stekly, J.L. Zar, IEEE Trans. Nucl. Sci., 12, 367-372, 1965.

## Slide 35: Heat balance (ideal case)
generation
cooling
stable
cryostable
not cryostable
not cryostable
constant heat transfer to the helium

## Slide 36: Heat balance (real case)
generation
cooling
stable
cryostable
not cryostable
not cryostable
boiling heat transfer to the helium

## Slide 37: Stekly-
Stekly cryostability condition:
can be formulated as Stekly  1 :
maximum cryostable operating current IStekly:

## Slide 38: Plan of the lecture
training and degradation
perturbation spectrum overview
heat balance
    Joule heating
    cooling and heat transfer
stability criteria
    enthalpy stabilization
    cryostability
    cold end recovery and the equal-area theorem
    meta-stable conductors:
      well-cooled operation in CICC’s
      MPZ and MQE

## Slide 39: Cold-end effects
What is the contribution of heat conduction ? Request steady state stability in all conditions:
assume that the normal zone is long and in equilibrium

## Slide 40: Equal-area theorem
introduce a new variable S:
B.J. Maddock, G.B. James, W.T. Norris, Cryogenics, 9, 261-273, 1969.
Sop = 0 Seq = 0
wh (T-Top)
A/w q’’’J
T
x
Tc
Tcs
Teq
Top
q’’
x

## Slide 41: Equal area theorem (ideal case)
no net area between generation and cooling curves !

## Slide 42: Equal area theorem (real case)
A/w q’’’J
wh (T-Top)

## Slide 43: Plan of the lecture
training and degradation
perturbation spectrum overview
heat balance
    Joule heating
    cooling and heat transfer
stability criteria
    enthalpy stabilization
    cryostability
    cold end recovery and the equal-area theorem
    meta-stable conductors:
      well-cooled operation in CICC’s
      MPZ and MQE

## Slide 44: Meta-stable conductors
adiabatically stabilized conductors:
  high Jop (good for cost)
  small Q’’’ (bad for large magnets)
cryo-stabilized conductors:
  large Q’’’, ideally infinite (good for large magnets)
  low Jop (bad for cost)
is there a compromise ?

## Slide 45: Idea-1: helium !

## Slide 46: ICS’s and CICC’s
M.O. Hoenig, Y. Iwasa, D.B. Montgomery,
Proc. 5th Magn. Tech. Conf., Frascati, 519, (1975)

## Slide 47: Heat balance for CICC’s
conductor temperature:
but the helium temperature evolves as well:
under which conditions the heat capacity is effectively used ?
  NOTE: at large enough h, TThe

## Slide 48: Stability of CICC’s
Q’’’
Iop
llim
helium + strand
heat capacity
strand
heat capacity
Joule heat
<
cooling
Joule heat
>
cooling
well-cooled
ill-cooled
balance of Joule heat and cooling at:
equivalent to Stekly = 1
In this case however the CICC is meta-stable as a large enough energy input will cause a quench !
J.W. Lue, J.R. Miller, L. Dresner, J. Appl. Phys., 51, 1, 772, (1980)
J.H. Schultz, J.V. Minervini, Proc. 9th Magn. Tech. Conf., Zurich , 643, (1985)

## Slide 49: Plan of the lecture
training and degradation
perturbation spectrum overview
heat balance
    Joule heating
    cooling and heat transfer
stability criteria
    enthalpy stabilization
    cryostability
    cold end recovery and the equal-area theorem
    meta-stable conductors:
      well-cooled operation in CICC’s
      MPZ and MQE

## Slide 50: Idea-2: heat conduction !
x
T
Tc
Tcs
T’eq
Top
x
q’’
wh (T-Top)
A/w q’’’J
S=0 at the boundaries (symmetry)
equal area still possible
but implies lower T’eq < Teq
Short normal zone

## Slide 51: Normal zone temperature
the corresponding temperature profile can be traced by numerical integration of the equal area balance:
x
T
q’’’J
M.N. Wilson, Y. Iwasa, Cryogenics, 18, 17-25, 1978

## Slide 52: MPZ
unstable equilibrium !
  temperature increase:
  generation > cooling
  
  thermal runaway
  temperature decrease:
  generation < cooling
  
  recovery
this is a Minimum Propagating Zone (MPZ)
the energy needed to form (instantaneously) a MPZ is the
Minimum Quench Energy (MQE) among all possible energies

## Slide 53: MQE
MQE provides lower boundary for energy margin vs. all possible situations
MQE allows verification of energy margin vs. perturbation spectrum, to:
  validate operation above the cryostable limits, and
  with energy margin larger than adiabatic limit
must be computed numerically
1-D
2-D
short heater
long heater
M.N. Wilson, Y. Iwasa, Cryogenics, 18, 17-25, 1978

## Slide 54: The general case…
CICC
Tapes and strands
Cables and braids
for
power transmission
Rutherford
induced flow,
transient heat transfer,
AC operation,
current distribution,
HTS,
coolants (N2, Ne, H2)…

## Slide 55: … and models…
things can get VERY complicated !

## Slide 56: …where to find out more
Papers and reviews:
    A.R. Krantowitz, Z.J.J. Stekly, A New Principle for the Construction of Stabilized Superconducting Coils, Applied Physics Letters, 6, 3, 56-57, 1965.
    P.F. Chester, Superconducting Magnets, Rep. Prog. Phys., XXX, Part II, 561-614, 1967.
    B.J. Maddock, G.B. James, W.T. Norris, Superconductive Composites: Heat Transfer and Steady State Stabilization, Cryogenics, 9, 261-273, 1969.
    M.N. Wilson, Y. Iwasa, Stability of Superconductors against Localized Disturbances of Limited Magnitude, Cryogenics, 18, 17-25, 1978.
    L. Dresner, Superconductor Stability 1983: a Review, Cryogenics, 24, 283, 1984.
Books:
    M.N. Wilson, Superconducting Magnets, Plenum Press, 1983.
    L. Dresner, Stability of Superconductors, Plenum Press, 1995.
    P.J. Lee ed., Engineering Superconductivity, J. Wiley & Sons, 2001.
    B. Seeber ed., Handbook of Applied Superconductivity, IoP, 1998.
    Y. Iwasa, Case Studies in Superconducting Magnets, Plenum Press, 1994.

## Slide 57
Some more difficult and special issues

## Slide 58: Ramp-rate effects
Quench current in SSC dipoles prototype showed a remarkable ramp-rate dependence:
  type A behaviour (continuous drop of Iq as f dI/dt)
  type B behaviour (initial jump of Iq followed by a flat dependence)
A. Devred, T. Ogitsu, Frontiers of Accelerator Magnet Technology, World Scientific, 184, 1996
type B
type A

## Slide 59: RRL in fusion magnets
 quench
 no quench
Pulsed fusion magnets showed significant ramp-rate limitation (RRL) much below rated current Irated
No RRL was observed below a limiting current Ilimiting
Irated
Ilimiting
M. Takayasu, et al., IEEE Trans. Appl. Sup., 3(1), 456, 1993.

## Slide 60: Flux-jumps
during a complete flux-jump the field profile in a superconducting filament becomes flat:
  e.g.: field profile in a fully penetrated superconducting slab
  energy stored in the magnetic field profile:
D = 50 m, Jc = 5000 A/mm2
Q’’’  3 mJ/cm3
area lost during flux jump

## Slide 61: Mechanical events
a strand carrying a current Iop in a field Bop is subjected to a force F
force per unit length acting on the strand F’ :
Jop = 400 A/mm2, Bop = 10 T  f = 4 GN/m3
a displacement  of a length l requires a work W :
 = 10 m, l = 1 mm  W’’’  40 mJ/cm3
Iop
Bop

Q’’’  1…10 mJ/cm3
l

## Slide 62: AC loss
a changing magnetic field causes persistent and coupling currents in a superconducting cable
these currents cause hysteresis or coupling AC loss
e.g. coupling current loss due to a field ramp
n = 100 ms, dB/dt = 1 T/s, B = 1 T
Q’’’  80 mJ/cm3
dB/dt

## Slide 63: Joule heating (cont’d)

## Slide 64: Forced-flow heat transfer
modified Dittus-Boelter-Giarratano-Yaskin correlation
  adapted coefficient
  correction for large surface temperature differences

## Slide 65: Superfluid helium heat transfer
heat transfer is usually limited by the Kapitza resistance at the surface:
n=3…4
=200…400 W/m2Kn
h equivalent (n=4):

## Slide 66: Heat flux limits

## Slide 67: Measured stability of a CICC
well-cooled regime
ill-cooled regime
st =4 10-10 m
Ast = 1.93 mm2
w = 9.4 mm
h=1875 W/m2K !
Tc = 6.2 K
Top= 4.5 K
vHe=0
Ilim = 380 A
Q’’’ induces flow v in helium and affects h:
if Q’’’ v h
if Q’’’ v h
dual stability

## Slide 68: CICC’s in superfluid Helium
… until the -transition from He-II to He-I (i.e. about 200 mJ/cm3 of helium, Q’’’ obtained scaling by fhe)…
in He-II h is higher (Kapitza resistance) thus increasing Ilim…
a dramatic effect is observed on stability as soon as the CICC is operated in superfluid Helium
… and in practice no effect for higher temperatures (corresponding to larger Q’’’)

## Slide 69: Stability examples
MRI magnets
BEBC

## Slide 70: Adiabatic stability: MRI magnet
Bop = 2 (T)
Top = 4.2 (K)
Iop = 400 (A)
Ic = Jc*ANbTi = 1650 (A)
fop = Iop/Ic = 0.24
Tcs = 7.6 (K)
fst =0.83, fsc =0.17
R 800
2000
NbTi wire
1 mm x 2 mm
Cu:NbTi=5
Jc 5000 A/mm2
Tc = 8.7 K
Q’’’=13 mJ/cm3

## Slide 71: Adiabatic stability: MRI magnet
Q’’’=13 mJ/cm3
…careful,
careful…

## Slide 72: Cryostability: the BEBC magnet
Bop = 5.1 (T)
Top = 4.2 (K)
Iop = 5700 (A)
st = 3.4 10-10 (m)
Ast = 176.5 (mm2)
w = 61 (mm)
Tcs = 7.4 (K)
h=600 (W/m2K)
800 MJ !
Stekly=0.55

## Slide 73: Cryostability: the BEBC magnet

## Slide 74: Equal area: the BEBC magnet
find maximum Iop satisfying the Equal Area condition with:
Iop = 7650 A
Bop = 6.8 T