## Slide 1: THE Model for Superconducting Cables
Luca Bottura(1), Cristina Rosso (2) and Marco Breschi (3)
(1) CERN, Switzerland
(2) CryoSoft, France
(3) University of Bologna, Italy

## Slide 2: Overview
Introduction
Description of THE Model
Time scales
Matrix form and solution algorithm
An example of application
Conclusions and perspective

## Slide 3: Introduction-1
Heating induced flow
mass flow
Reynolds
stability margin
The stability margin is
largely independent on
mass-flow: the heat transfer
is greatly enhanced by energy
deposition from the strands
J.W.Lue, J.R.Miller, L.Dresner
J. Appl. Phys., 51, 1, 1980

## Slide 4: Introduction-2
Flow coupling and train effects
time
helium temperature
Velocity shear and heat transfer
between flows give rise to a
temperature train similar to a
Taylor-Aris dispersion
The Quench Experiment on Long Length
Final Report, EPFL/JAERI/SINTEZ/MIT-PFC, 1997

## Slide 5: Introduction-3
Ramp-rate limitation
ramp-time
quench current
The quench current of a coil
is significantly affected by
the ramp-rate and powering
history
M. Takayasu, et al., IEEE Trans. Appl.
Sup., 3(1), 456-459, 1993

## Slide 6: Introduction-4
Super-currents and BICC’s
L.Krempasky, C. Schmidt
Cryogenics, 39, 23-33, 1999
supercurrent
time
Large, long lasting currents
(supercurrents) are caused
by transposition errors w/r
to external field changes

## Slide 7: Introduction-5
MQE of triplets
The balance of current and
heat transfer causes a sharp
transition (kink) from single
strand to multiple strand
behaviour
N. Amemiya, et al.
Cryogenics, 38, 559-568, 1998
stability margin
fraction I/Ic

## Slide 8: THE Generic Cable

## Slide 9: Three Coupled Fields
Thermal
- strands
- structure
- insulation
- …
Hydraulic
- helium
- LN2
- neon
- …
Electric
- strands
- stabilizer
- shunts
- …

## Slide 10: Thermal Model - 1
solid temperature Ti
heat exchange among solids
heat exchange with coolants
Joule heat
N parallel, 1-D thermal solids

## Slide 11: Thermal Model - 2
Non-linear material properties
  heat capacity
  thermal conductivity
Non-linear heat generation (Joule heat) in superconducting materials
Variable cross section along the length x

## Slide 12: Hydraulic Model - 1
temperature
mass, momentum, and energy transfer
heat exchange with pipe wall
volumetric flux Vh=vhAh
H parallel, 1-D compressible flow pipes
pressure
pipe wall friction
counter-flow in helium-II

## Slide 13: Hydraulic Model - 2
Exact description of 1-D compressible flow
  low and high Reynolds flow conditions
  shocks
  arbitrary fluid (He, LN2, Neon, …)
Variable cross section and channel geometry along the length x
Empirical correlations for h and f

## Slide 14: Electric Model - 1
strand current
external voltages (e.g. dB/dt)
inter-strand conductance matrix
inductance matrix
parallel resistance matrix
E parallel, 1-D current carrying conductors

## Slide 15: Electric Model - 2
Non-linear parallel resistance (e.g. strand during quench)
Variable properties along the length x
  inter-strand inductance (cable geometry)
  inter-strand conductance (localised vs. smeared contacts)
  voltage (field profile)

## Slide 16: Coupling of the Fields - 1
p
t
Thermal  Thermal
  thermal resistance Hij
    computed for intimate contact (e.g. soldered)
    unknown for simple contact, can be estimated using electrical resistance Rij
Wiedemann-Franz-Lorenz law

## Slide 17: Coupling of the Fields - 2
Thermal  Hydraulic
  wetted perimeter pih
  heat transfer coefficient hih
    established correlations provide a good estimate
    details not settled (experimental work)
      phase transitions
      induced flow
      large T
      complex geometry and dimensional effects

## Slide 18: Coupling of the Fields - 3
Hydraulic  Hydraulic
  wetted perimeter phk and perforation hk
  heat transfer coefficient hhk
    order-of-magnitude correlations for perforated pipes
    little relevant measurements available
  transverse massflow mhk
    no relevant measurements available
    assumption

## Slide 19: Coupling of the Fields - 4
Electric  Electric
  interstrand resistance Ref
    intense experimental work, relevant for AC loss
    order-of-magnitude predicted at design
    controlled at production
  inductance lef
    from classical electrodynamics

## Slide 20: Coupling of the Fields - 5
Thermal  Electric
  strand resistivity i
    measured
    satisfactory understanding of macroscopic behaviour of superconducting strand
electric field
current in the superconductor

## Slide 21: Time Scales

## Slide 22: Matrix Form
All THE equations can be written as:
unknowns
Ti
vh
ph
Th
Ie
convection
diffusion
source
Parabolic-Hyperbolic system of PDE’s

## Slide 23: Solution Algorithm - 1
Variable order Finite Elements in space
    2 nodes (linear)  6 nodes (quintic)
    best compromise: 3 nodes (parabolic)
Variable order, multi-stage, implicit time integration (Beam-Warming class)
    Euler bwd (1st order)  Adams (3rd order)
    HO correction up to 4th order
    automatic error and step control (step halving)
    best compromise: Crank-Nicolson (2nd order)

## Slide 24: Solution Algorithm - 2
Why high order of accuracy (time) and interpolation (space) ?
p
t
L=1m
T0 = 300 K
p0 = 1 bar
p = 0.2 bar

## Slide 25: Solution Algorithm - 3

## Slide 26: An Example of Application
2-strands cable
10 mm twist pitch
1.6 m long
resistive heater
40 mm long
transposition fault (70 mm2 flux loop)
4.2 K, 1 bar
helium bath
Courtesy of C. Schmidt, FzK

## Slide 27: Simulations
5 components model
      2 thermal NbTi/Cu strands, coupled to electrical strands
      2 electrical NbTi/Cu strands, coupled to thermal strands
      1 helium channel (large x-section, negligible flow)
simulation
      uniform mesh
        1500 linear, 2 nodes elements (dx  1.5 mm)
        500 parabolic, 3 nodes elements (dx  2 mm)
      adaptive, implicit 2nd order time integration algorithm
      20 s real time  2’ to 10’ CPU time on DEC-Alpha ws

## Slide 28: Field Ramp w/o Quench - 1
symmetry line  dI/dx = 0
flux loop
boundary  I= 0

## Slide 29: Field Ramp w/o Quench - 2

## Slide 30: Field Ramp and Quench - 1

## Slide 31: Field Ramp and Quench - 2

## Slide 32: Field Ramp and Quench - 3

## Slide 33: Conclusions - Achievement
THE model is:
  comprehensive
    1-D (exact) representation of THE 3-D topology
    covers THE coupled fields
  flexible
    arbitrary combination of THE components
    arbitrary non-linearity
  manageable

## Slide 34: Conclusions - Applications
Large range of applications:
      detailed stability and quench propagation, including current distribution
      AC loss in cables taking including saturation effects
      current diffusion and temperature profiles in joints and adjacent cable
      parallel cooling of cables in a coil
      current leads
      …
any situation obtained assembling
THE components

## Slide 35: Conclusions - Perspective
Applications:
    validation vs. experimental data
    studies on cable geometry other than CICC’s
    new fluids (nitrogen, neon, …)
    new SC materials (HTc tapes)
Development:
    Space p-h adaptivity
      error estimate (front tracking and Z2 error estimate)
      automated mesh generation for HO-FE’s